|  |
| --- |
| DoP-Nr.: 1725 0000 |
| **Declaration of Performance**  According to annex lll of Regulation (EU) 305/2011 (construction products regulation)  date: 05-06-2013 |

|  |  |  |
| --- | --- | --- |
| **1.** | Unique identification code of the product-type | Bauder Plant E 4mm |
| **2.** | Type, batch or serial number allowing identification of the construction product as required pursuant to Article 11 (4) | see product label |
| **3.** | Intended use | Reinforced bitumen sheets for roof waterproofing  Bitumen damp proof sheet including basement tanking sheets |
| **4.** | Name, registered trade name or registered trade mark and contact address of the manufacturer as required pursuant to Article 11 (5) | Paul Bauder GmbH & Co. KG,  Korntaler Landstrasse 63, 70499 Stuttgart  Germany |
| **5.** | Where applicable, name and contact address of the authorised representative whose mandate covers the tasks specified in Article 12 (2) | Not relevant |
| **6.** | System or systems of assessment and verification of constancy of performance of the construction product as set out in Annex V | System 2+ |
| **7.** | In case of the declaration of performance concerning a construction product covered by a harmonised standard | 1724-CPR-021101 / 021201 / 022101 / 022201 |
| **8.** | In case of the declaration of performance concerning a construction product for which a European Technical Assessment has been issued | Not relevant |

**9. Declared performance**

|  |  |  |
| --- | --- | --- |
| **Essential characteristics** | **Performance** | **Specification** |
| Reaction to fire | E | EN 13707  EN 13969 |
| Watertightness type B | passed |
| Tensile properties: :  Max. Tensile force lenght (N/50 mm)  Max. Tensile force transverse (N/50 mm)  Elongation at max. tensile force lenght ( %)  Elongation at max. tensile force transverse ( %) | -  1000  1000  ≥ 45  ≥ 45 |
| Flexibility at low temperature (°C) | ≤ -36 |
| Hazardous Substances **b), c)** | Passed  , see 5.3 EN 13707  see 5.15 EN 13969 |


For all other characteristics according to EN 13707 and EN 13969: NPD (no performance determined)

a) Determination of external fire performance is a system test. which can be influenced by system components, which are not produced or sold by Bauder GmbH, thus performance for each product can not be given.

b) Product does not contain asbestos or tar

c) Because there is no European test method for leaching of the products, no statement can be made

Signed for and on behalf of the manufacturer by:

Dr. Peter Wagner, Plant Manager Stuttgart

Stuttgart, 01.07.2013 .....................................................................................................

(signature)