DECLARATION OF PERFORMANCE

| No: | 13189450 |
| --- | --- |
| 1. Unique identification code of the product-type: | Bauder JFRI Inverted Insulation Grades EPS 200 and 300 |
| 2. Type, batch or serial number or any other element allowing identification of the construction product as required pursuant to Article 11(4) of the CPR: | Bauder JFRI |
| 3. Intended use or uses of the construction product, in accordance with the harmonised technical specification, as foreseen by the manufacturer: | Shape moulded, modified beads of EPS insulation for use on inverted roofs |
| 4. Name, registered trade name or registered trade mark and contact address of the manufacturer as required pursuant to Article 11(5): | Bauder Ltd 70 Landseer Road Ipswich Suffolk IP3 0DH |
| 5. Where applicable, name and contact address of the authorised representative whose mandate covers the tasks specified in Article 12(2): | Not Applicable |
| 6. System or systems of assessment and verification of constancy of performance of the construction product as set out in Annex V: | AVCP System 3 |
| 7. In case of the declaration of performance of the construction product covered by a harmonised standard: - name and number of notified body: | British Board of Agrément; BRE (RtF) |
| - performed: | Reaction to Fire Thermal Conductivity Compressive Strength |
| - under system: | System 3 |
| - and issued: | Test report on application |

Declared Performance

| Essential Characteristic | Performance | Harmonised technical standard |
| --- | --- | --- |
| Length and width | L2 & W2 | BS EN 13163:2012 |
| Thickness | T2 |  |
| Squareness | S2 |  |
| Flatness | P5 |  |
| Reaction to Fire | Euroclass E | BS EN 13501-1:2007 |
| Thermal Conductivity - Declared | 0.033W/mK | BS EN 13163:2012 |
| Thermal Resistance | See table 3 | BS EN 13163:2012 |
| Compressive Strength at 10% deformation | 200 & 300 kN/m2 | BS EN 12086:2013 |
| Compressive Creep | CC(2/1.5/50)60 CC(2/1.5/50)90 | BS EN 1603:2013 |
| Deformation under specified compressive load and temperature | 5% | BS EN 1605:1997 |
| Dimensional stability | DS(70,90)1 | BS EN 1604:1997 |
| Long-term water absorption by diffusion | WD(V)3 | BS EN 12088:1997 |
| Long-term water absorption by immersion | WL(T)2 | BS EN 12087:1997 |
| Thickness | 100mm – 250mm in 5mm increments | BS EN 823:2013 |
| Chemical resistance | On application | - |
| Compatibility with other components | On application | - |

Table 3 - Thermal Resistance m2K/W

| Nominal Thickness mm | Thermal Resistance m2K/W Declared |
| --- | --- |
| 50 | 1.5152 |
| 100 | 3.0303 |
| 105 | 3.1818 |
| 110 | 3.3333 |
| 115 | 3.4848 |
| 120 | 3.6364 |
| 125 | 3.7879 |
| 130 | 3.9394 |
| 135 | 4.0909 |
| 140 | 4.2424 |
| 145 | 4.3939 |
| 150 | 4.5455 |
| 155 | 4.6970 |
| 160 | 4.8485 |
| 165 | 5.0000 |
| 170 | 5.1515 |
| 175 | 5.3030 |
| 180 | 5.4545 |
| 185 | 5.6061 |
| 190 | 5.7576 |
| 195 | 5.9091 |
| 200 | 6.0606 |
| 205 | 6.2121 |
| 210 | 6.3636 |
| 215 | 6.5152 |
| 220 | 6.6667 |
| 225 | 6.8182 |
| 230 | 6.9697 |
| 235 | 7.1212 |
| 240 | 7.2727 |
| 245 | 7.4242 |
| 250 | 7.5758 |

The performance of the product identified in points 1 and 2 is in conformity with the declared performance.

This declaration of performance is issued under the sole responsibility of the manufacturer identified in point 4.

On behalf of the manufacturer by:	Date of Issue:

Paul Felgate, R&D Manager	1st July 2013